Holographic studies of photoinduced anisotropy in molecular glassy films containing diphenylamine based azochromophores
Andris Ozols, Valdis Kokars, Peteris Augustovs, Kaspars Traskovskis, Dmitry Saharov
Faculty of Material Science and Applied Chemistry, Riga Technical University, Latvia
e-mail: aozols@latnet.lv
Photoinduced anisotropy (PA) is experimentally studied in  three molecular glassy films synthesized in our Faculty and containing diphenylamine based azochromophores {4-((4-nitrophenyl)diazenyl)-N-(4-((4-nitrophenyl)diazenyl)phenyl)-N-(2-trityloxy)ethyl) benzeneamine (shortly K-D-24), 4-((2-chloro-4-tritylphenyl)diazenyl)-N-(4-((2-chloro-4-tritylphenyl)diazenyl)phenyl)-N-(2-(trityloxy)ethyl)benzenamine (shortly K-D-25) , 4,4'-(2-(trityloxy)ethylazanediyl)bis(4,1-phenylene)bis(diazene-2,1-diyl)dibenzonitrile (shortly K-D-32) } and, for comparison, in an a-As2S3 film. Holographic method enabling simultaneous measurements of s- and p-polarized diffracted light powers proposed in Ref.[1] was applied in both transmission and reflection modes. Holographic grating recording with the period of 2 μm was made by two equally strong 532 nm  p- polarized laser beams with total light intensity of 0.81 W/cm2. The readout was made by 633 nm circularly polarized  beam, and the s- and p-polarized components of diffracted light were separated by Glan-Thompson prism.

PA was characterized by diffraction efficiency difference (DED), ηs – ηp , and by anisotropy contrast A = (ηs – ηp)/(ηs + ηp). Corrections of the results were made taking into account the inherent anisotropy of HG  and the anisotropy of Fresnel reflection losses [2]. DED exhibited markedly different kinetic behavior in transmission and reflection modes. There was a  deep negative minimum in transmission mode in all samples, and a growth with oscillations up to saturation in reflection mode. Small initial DED maxima were specific to a-As2S3 film. The highest PA was found in K-D-24 film in transmission mode (A=-0.23) and in K-D-25 film (A=0.49).The photoinduced refractive index difference, |ns-np| absolute values of the studied samples were estimated to vary in the 0-0.24 range. The obtained results can be explained in terms of trans-cis photoisomerisation (K-D films) and photooriented bond switching (a-As2S3) accompanied by other processes.
References

1. A.Ogiwara, H.Kakiuchida, M.Tazawa, and H.Ono, Jap.J.Appl.Phys. 11, 7341 (2007).

2. A.Ozols and M.Reinfelde, Proc.SPIE 5123, 133 (2003).






