Riga Technical University 53rd International Scientific Conference dedicated to the 150th anniversary and

The 1st Congress of World Engineers and Riga Polytechnical Institute / RTU Alumni

“Trityloxyethyl and tert-butyl groups containing molecular glasses of 4H-pyran-4-ylidene derivatives with light-emitting and amplified spontaneous emission properties”
Elmars Zarins1 (Riga Technical University, Institute of Applied Chemistry)1, Aivars Vembris2, (Institute of Solid State Physics, University of Latvia)2, Karina Siltane1, Elina Misina1, Valdis Kokars1, Kristine Lazdovica1, Santa Popova2, Valdis Kampars1, Martins Rutkis2.
Keywords – OLED, organic glass forming compounds, 2-tert-butyl-6-methyl-4H-pyran-4-one, fluorescent dye.
I. Introduction
Dyes which make amorphous structure by deposited from volatile organic solvents and having good light-emission properties show potential in organic photonics. One of the methods for obtaining such molecular glasses from organic compounds is incorporation of trityloxyethyl groups in their molecules [1]. In our previous research we successfully obtained glass forming derivatives of pyranylidene using 2,6-dimethyl-4H-pyran-4-one as starting material. However, due to its two activated methyl groups, in further reactions with trityloxyethyl group containing aromatic aldehyde, a mixture of mono- and bis- condensation products were obtained, which separation was complicated [1-2]. Nevertheless, each of products was separated and purified, however their yields were low. Starting synthetic procedure from 2-tert-butyl-6-methyl-4H-pyran-4-one not only prevent this problem as only one activated methyl group is in its molecule, but also enhances the formation of amorphous structure of target compounds [3]. In this report we will describe our findings of trityloxyethyl group containing molecular glasses based on 2-tert-butyl-6-styryl-4H-pyran-4-one.
II. SYNTHESIS AND PHYSICAL PROPERTIES
Light-emitting amorphous glasses containing 2-tert-butyl-6-styryl-4H-pyran-4-ylidene fragment have been synthesized according the schema showed below and obtained in good yields up to 51% after separation and purification by liquid column chromatography.  Compounds 1a-d have been obtained from 2-tert-butyl-6-methyl-4H-pyran-4-one. 
[image: image1.wmf]O

A

H

3

C

1

a

-

d

C

H

3

C

H

3

C

H

3

H

O

N

O

O

P

h

P

h

P

h

P

h

P

h

P

h

2

N

O

O

P

h

P

h

P

h

P

h

P

h

P

h

O

A

O

O

N

N

O

O

O

H

H

N

N

A

=

;

;

Z

W

K

-

1

T

B

F

o

r

1

a

a

n

d

Z

W

K

-

1

T

B

F

o

r

1

b

a

n

d

D

W

K

-

1

T

B

F

o

r

1

c

a

n

d

J

W

K

-

1

T

B

D

W

K

-

1

T

B

J

W

K

-

1

T

B

K

W

K

-

1

T

B

C

H

3

C

H

3

C

H

3

N

;

F

o

r

1

d

a

n

d

K

W

K

-

1

T

B

O

O

E

t

P

y

P

i

p

e

r

i

d

i

n

e

1

7

-

5

1

%

All glasses show good thermal stability with thermal decomposition temperatures from 264o to 318oC and glass transition values up to 158oC for DWK-1TB. Their physical properties  will be discussed in detail during the conference.
III. CONCLUSIONS

The synthesized compounds ZWK-1TB, DWK-1TB, JWK-1TB and KWK-1TB, which contain trityloxyethyl and tert-butyl groups form a glassy structure in the solid state from volatile organic solvents. By starting synthesis from 2-tert-butyl-6-methyl-4H-pyran-4-one, not only the yield of target compounds have been improved, but they also have better thermal properties compared to similar pyranylidene type compounds published previously by us [1].
IV. ACKNOWLEDGEMENTS

This work has been supported by the European Social Fund within the project «Support for the implementation of doctoral studies at Riga Technical University».
V. References

[1] A. Vembris, E. Zarins, J. Jubels, V. Kokars, I. Muzikante, A. Miasojedovas and S. Jursenas, Thermal and Optical properties of red luminescent glass forming symmetric and non symmetric styryl-4H-pyran-4-ylidene fragment containing derivatives. Opt. Mater., Vol 34(9), 2012, pp. 1501-1506.
[2] E. Zarins, J. Jubels and V. Kokars. Synthesis of red luminescent non symmetric styryl-4H-pyran-4-ylidene fragment containing derivatives for organic light-emitting diodes. Adv. Mater. Res., Vol 222, 2011, pp. 271-274.
[3] E. Zarins, K. Siltane, E. Misina, V. Kokars, K. Lazdovica, A. Vembris, V. Kampars, I. Muzikante and M. Rutkis, Synthesis, optical and thermal properties of glassy trityl group containing derivatives of 2-tert-butyl-6- methyl-4H-pyran-4-one. Proc. SPIE, Vol 8435, 2012, pp. 84351Q-1-84351Q-7. 
� EMBED ChemDraw.Document.6.0  ���








PAGE  

[image: image2.wmf]O

A

H

3

C

1

a

-

d

C

H

3

C

H

3

C

H

3

H

O

N

O

O

P

h

P

h

P

h

P

h

P

h

P

h

2

N

O

O

P

h

P

h

P

h

P

h

P

h

P

h

O

A

O

O

N

N

O

O

O

H

H

N

N

A

=

;

;

Z

W

K

-

1

T

B

F

o

r

1

a

a

n

d

Z

W

K

-

1

T

B

F

o

r

1

b

a

n

d

D

W

K

-

1

T

B

F

o

r

1

c

a

n

d

J

W

K

-

1

T

B

D

W

K

-

1

T

B

J

W

K

-

1

T

B

K

W

K

-

1

T

B

C

H

3

C

H

3

C

H

3

N

;

F

o

r

1

d

a

n

d

K

W

K

-

1

T

B

O

O

E

t

P

y

P

i

p

e

r

i

d

i

n

e

1

7

-

5

1

%

_1400436029.cdx

