[image: image1.wmf] 


[image: image2.jpg]



OPTIMIZATION OF SMART CLOTHES SYSTEM 
Ingrida Sahta1, Mg. sc. ing., Ilze Baltina2, Dr. sc. ing., Juris Blums3, Dr. phys 
1-2Riga Technical University, Institute of Textile Material Technologies and Design, Riga, LATVIA
3Riga Technical University, Institute of Technical Physics, Riga, LATVIA
Corresponding author: Ingrida Sahta, ingrida.sahta@rtu.lv
Key words: Smart Clothes, Microclimate, Electrical System, Solar cells, Peltier elements 
1. ABSTRACT
The garment with integrated Peltier elements is one of the human microclimate regulatory solution. [1]

It is known already discovered and patented smart clothes and other articles, with integrated thermoelectric converters. Here should be mentioned articles with several thermoelectric modules [2]; with integrated heat exchanger with piping system [3] and with air conditioners [5]. Systems differ in terms of power source selection; both of the solution the heat removal from thermoelectrical module cold side, but also of the cooling type the warm side. 
The research is dedicated to microclimate regulatory vest with an integrated electrical system, which is also composed Peltier elements, and cooling function is based on the heat conductivity in solids [4]. In the experiments with thermoelectric modules - Peltier elements - and the different thickness of copper, bronze and steel threads and different density fabrics, as well as copper foil, it is observed that the copper foil provides the necessary heat removal, which, in turn, provides favourable conditions for the cooling.
To verify microclimate regulatory vests compliance with the general requirements of article, it is scheduled an assessment at physiologically - hygienic point of wearing by the appropriate operating conditions.

In assessing the model to meet the general requirements to be raised smart clothes, it is concluded that currently the existing system configuration is relatively little provided the clothing comfort, because the parts are robust, their compounds are unstable, the used materials are hard and inflexible, and they do not represent the textile or equivalent products. All the components have to be removed before the product cleaning, because they are not secured against the effect of moisture.

2. References

1. Bansevičius R, Račkiene R, Virbalis J. A. (2007). The body Cooling System Integrated into the Clothes. Electronics and electrical engineering. - 2007. - No. 5 (77). – S. 3-6
2. Martin R. Temperature regulated clothing (2004). United States Patent No: US 7,186,957 B2, Reg. – 06.08.2003 10/636,511, publication: US 2004/0118831 A1 24.06.2004, Int. Cl. H05B 3/34

3. Saunders J., Jacob J. D., Gao D., Myers M. A. Thermoelectric modules and a heating and cooling apparatus incorporating same (2003). United States Patent No: US 6,739,138 B2, Reg. – 02.07.2002 10/186,618, publication: US 2003/0097845 29.05.2003, Int. Cl. F25B 21/02

4. Weidner R.T. (1985). Physic, Allyn and Bacon, USA, 961 p.
5. Zhixinn Li. Air conditioner for flexible material-based devices (2004). United States Patent No: US 6,823,678 B1, Reg. – 22.12.2003 10/743,640, publication: 30.11.2004, Int. Cl. F25B 21/02
� EMBED Word.Picture.8  ���





��



Annals Of The Oradea University.  Fascicle Of Textile- Leatherwork





INTERNATIONAL SCIENTIFIC CONFERENCE


"Innovative solutions for sustainable development of textiles industry"


Oradea 2010 


�
�












PAGE  
1

[image: image3.wmf] 

_1321012879.doc
[image: image1.png]






